## Slide 1
CLATHRATES BASED ON HYALURONIC ACID
Development of viscoelastic materials for
osteoarticular application
Gilda De Luca, Davide Renier, Günter Kirschner
idea PATENTED by L. Šoltés et al., EP 1272530

## Slide 2: Objectives of the project
To develop novel HA materials whose rheological properties would result from the formation of a clathrate.
This result can be achieved by:
  preparation of -cyclodextrin (-CD) derivative of HA
  preparation of adamantane derivative of HA
The association of the two HA derivatives should lead to in situ formation of a polymeric network with enhanced viscoelastic properties.

## Slide 3
Synthesis of HA-cyclodextrin derivative
Direct esterification
HA-COOH + HO-CD → HA-COO-CD
Introduction of a spacer e.g. 3-hydroxypropionic acid
HA-COOH + HO-CH2CH2COOH + HO-CD → HA-COO-CH2CH2COO-CD

## Slide 4
Synthesis of HA-adamantane derivative
Formation of amide
HA-COOH + ADAM-NH2 → HA-CONH-ADAM
Degree of substitution (DS) about 2.5 – 5 %
Products are soluble in water

## Slide 5
HA-adamantane derivative, DS = 2.5 %
HA in HA-adamantane (600 kDa)
Dynamic viscosity of the aqueous solution 9.82 mg/ml at a shear rate 1 s-1 = 60.80 Pa
HA sodium salt 600 kDa
Dynamic viscosity of the aqueous solution 14.1 mg/ml at a shear rate 1 s-1 = 0.40 Pa

## Slide 7
Applications
tissue regeneration
improvement of the rheological
characteristics of synovial fluid
ophthalmic surgery
drug carrier

## Slide 8: Advantages of the technology
Formation of the gel in situ (intra-articularly)
Possibility to deliver - within the solution of the HA-cyclodextrin derivative - pharmacologically active molecules, e.g. NSAID, antioxidant (released at the moment of formation of the clathrate)

## Slide 10: Preliminary conclusions
Novel HA-CD derivatives were prepared by direct esterification or through insertion of a spacer.
HA-adamantane derivative was prepared with dynamic viscosity characteristics superior to those of native HA.

## Slide 11: Future activities
Introduction of spacers of various
length between CD and HA or between
adamantane and HA in order to
facilitate formation of clathrates

## Slide 12: … recently published news

## Slide 13: … from our kitchen

## Slide 14: … from our kitchen

## Slide 15: … from our kitchen

## Slide 17: … from our kitchen
Effect of sodium naproxen on HA degradation induced by an artificial inflammation induced by
A) 0.1 μM CuCl2 plus 100 μ M ascorbic acid plus 50 μM H2O2 ► OH
B) 0.1 μM CuCl2 plus 100 μM ascorbic acid plus 2 mM NaOCl ► HOCl/-OCl

## Slide 18: … future approaches
… its function would be
  To block the association
  To protect the engineered tissue against oxidative damage
… and what about to apply an antioxidant
as the competitor?

## Slide 19
Thank you for your attention