## Slide 1
Study of antioxidative properties of natural and synthetic substances on high-molecular-weight hyaluronan degradation in vitro.
The main investigators: Dipl.- Chem. M. Stankovská
Dipl.- Chem. L. Šoltés, DrSc.
Dipl.- Chem. P.Gemeiner, DrSc.
Institute of Experimental Pharmacology, Slovak Academy of Sciences, Bratislava, Slovakia
Institute of Chemistry, Slovak Academy of Sciences, Bratislava, Slovakia
Cooperation with: Doc.Dipl.- Chem. V. Brezová
Dipl. - Chem. J. Rýchly, DrSc.
Dipl. - Chem. V. Sasinková
ZA. H. Spalteholz, PhD.
Prof. Dr. J. Arnhold
Faculty of Chemistry and Food Technology, Slovak Technik University, Bratislava, Slovakia
Polymer Institute, Slovak Academy of Sciences, Bratislava, Slovakia
Institute of Medical Physics and Biophysics, University of Leipzig, Germany

## Slide 2: Composition of joint

## Slide 3: Synovial fluid
Ultrafiltrate of blood plasma: HA, glycoproteins.
Function of HA: lubricant, shock - absorber, trapper of potential damage molecules

## Slide 4: Hyaluronan HA is composed from disaccharid units of glucuronic acid and N-acetylglucosamine, connected with β(1-3) a β(1-4) glycosidic bonds

## Slide 5: Degradation of HA in synovial fluid
Damage of synoviocytes
Fragments of degraded HA act proinflammatory and immunostimulatory

## Slide 7: Possible peroxynitrite reactions

## Slide 8: Mechanism of damage by HOCl/-OCl

## Slide 9: Kinetics of hyaluronan degradation and its inhibition by ibuprofen and stobadin
HPLC
Capillary viscometry

## Slide 10: Brookfield DV-II+ viscometer

## Slide 11: Viscometric cup and spindle

## Slide 12: Study of HA degradation in vitro
Oxidative species: O2, H2O2, H2O2+ Cu2+, HOCl, ONOO-.
Methods:
1. rotational viscometry (primary)
2. IR, UV-VIS spectroscopy, EPR, TGA, DSC, CL (secondary)

## Slide 13: Material and Methods
HA (2.5 mg/ml) is swollen a dissolved 24 hours in 0.15 M NaCl solution. Sample is stored in dark.
Stock solutions H2O2, CuCl2 , ascorbic acid and HOCl are prepared in 0.15 M NaCl solution.
Measurement conditions are: 250C, 180 rpm, the first measurement begins 2 min. after reaction onset. Intervals of measurements: 3 min.
Hyaluronan degradation is termed by precipitation in 20 ml 96% etanol.
After 24 hours storage in the fridge precipitate is sedimented and sediment is decanted by 20 ml 96% ethanol. The sample is sedimented and dried up in exikator.

## Slide 14: Hypoxia and reoxygenation in the joint

## Slide 15: Reactions in healthy joint
Mn + + O2 → M(n+1)+ + •O2-
M(n+1)+ + ascorbic acid → Mn + + oxidized ascorbic acid
•O2- + •O2- + 4 H+ → 2 H2O2
H2O2 + Mn + → M(n+1)+ + HO- + •OH
HA + •OH → fragmentation

## Slide 16: Reaction H2O2 + CuCl2
Cu2+ + H2O2 → Cu+ + [•O2- + H+] + H +
Cu+ + H2O2 → Cu2+ + •OH + HO-
•O2- + H2O2 → O2 + •OH + HO-

## Slide 17: Time course of 30 EPR spectra
(DMPO spin trapping agent)
a, c(CuCl2) = 0 M
b) c(CuCl2) = 2.5 M

## Slide 18: Kinetics of the decrease in viscosity of a HA solution incubated with CuCl2 or H2O2

## Slide 19: Kinetics of the decrease in viscosity of a HA solution incubated with H2O2 + CuCl2

## Slide 20: Characterization of degraded HA by methods of IR and chemiluminometry

## Slide 21: Viscosity changes of hyaluronan in system CuCl2 + H2O2 + ascorbic acid

## Slide 22: Viscosity changes of hyaluronan after addition of HOCl

## Slide 23: Possible models for testing of antioxidative effects of substances

## Slide 24: Conclusion
The high - molecular - weight of HA and its rheological properties predeterminate this biopolymer to be an in vitro probe for study of effects of oxidative species on biopolymer as such, and for testing prooxidative or antioxidative behalf of different substances.
High – molecular - weight hyaluronan may contain traces of polyvalent metal cations (Fe2+, Cu1+, Cu2+…) which influence its degradation via Fenton reaction in the system with hydrogen peroxide.
The addition of H2O2 affects the hyaluronan degradation.
The system CuCl2 + H2O2 speeds up the degradation. Copper ions alone don´t influence the degradation. EPR with DMPO-spin trapping provided generation of •OH in this system.
On the other hand, the EPR spin trapping experiments performed in aerated DMSO/water mixed solvent (5:1; v/v) in the presence of hydrogen peroxide plus Cu2+ ions evidenced the generation of three DMPO-adducts attributed to DMPO-OOH, DMPO-OCH3 and DMPO-CH3.

## Slide 25
Addition of ascorbic acid in high concentration sped up the degradation. IR spectrum did not detect any oxo - groups.
The obtained results indicate that HA is degraded by HOCl only at high non-physiological concentrations. Its function in inflamed joints is probably primarily antimicrobial.
A different composition of degradative systems induces different chemical processes.
Rotational viscometry by means of inert material (Teflon) might be the most efficient analytical method in kinetics study of hyaluronan degradation.

## Slide 26: Publications
L. Šoltés, D. Lath, R. Mendici, P. Bystrický: Radical degradation of high molecular weight hyaluronan: Inhibition of the reaction by ibuprofen enantiomers. Methods Find. Exp. Clin. Pharmacol. 23(2), 2001, 65-71.
M. Stankovská, L. Šoltés, A. Vikartovská, R. Mendichi, D. Lath, M. Molnárová, and P. Gemeiner: Study of Hyaluronan Degradation by Means of Rotational Viscometry: Contribution of the Material of Viscometer. Chem.Papers 58 (5), 2004, 341-347.
M. Stankovská, L. Šoltés, A. Vikartovská, P. Gemeiner, G.Kogan and D. Bakoš: Degradation of high–molecular–weight hyaluronan: A rotational viscometry study. Biologia 2005, vol. 60, Suppl. 17., 149-152.
D. Lath, K. Csomorová, G. Kolláriková, M. Stankovská, L. Šoltés: Molar Mass–Intrinsic Viscosity Relationship of High-Molar-Mass Hyaluronans: Involvement of Shear Rate. Chem. Papers, 2005 – in press.
L.Šoltés, M. Stankovská, G.Kogan, P. Gemeiner, and R. Stern: Contribution of Oxidative-Reductive Reactions to High-Molecular-Weight Hyaluronan Catabolism. Chemistry and Biodiversity 2, 2005, 1242-1245.

## Slide 27: Lectures
M. Stankovská, L. Šoltés, D. Lath, A. Vikartovská, P. Gemeiner, G.Kogan, D. Bakoš: Degradation of high-molecular-weight hyaluronan: Viscometry measurements. 9 interdisciplinary slovak-czech toxikological conference, Píla-Častá, Slovak Republic, September 2004 + abstract in text-book.
M. Stankovská, L. Šoltés, A. Vikartovská, P. Gemeiner: Viscometry study of hyaluronan degradation in vitro. Švecov Memorial, Pharmaceutical Faculty, Bratislava, Slovak Republic, November 2004.
M. Stankovská, L. Šoltés, V. .Brezová, V. Sasinková, E. Hrabárová, P. Gemeiner: Study of oxidative damage of high-molecular-weight hyaluronan in the system CuCl2 + H2O2. 55. Pharmakological days, Hradec Králové, Czech Republic, September 2005, abstract in Česko-slovenská fyziologie.